- SECTION 02620

- SUBSURFACE DRAINAGE

- (SYNTHETIC DRAINAGE SYSTEM)

- PART 1 – GENERAL

1.01 SUMMARY

- Section includes:  Underdrain for Synthetic Turf System

- Related Sections:

  - Section 02610 – Pipe and Fittings

  - Section 02720 – Storm Sewer Systems

1.02 REFERENCES

- American Standard for Testing and Materials (ASTM)

  - ASTM D-1621 Standard Test Method for Compressive Strength of Drainage

Core

  - ASTM D-4716 Standard Test Method for Determining Flow Rate of

Underdrain

  - ASTM D-4491 Standard Test Method for Determining Permeability of Geotextile

  - ASTM D-4833 Standard Test Method for Determining Puncture Resistance of Geotextile

  - ASTM D-3786 Standard Test Method for Determining Burst Strength of Geotextile

  - ASTM D-4751 Standard Test Method for Determining Apparent Opening Size of Geotextile

  - ASTM D-4355  Standard Test Method for Determining Ultraviolet Resistance of Geotextile

1.03 DEFINITIONS

- Terms – Taken from ASTM D-4439

  - Geotextile:  Any permeable textile used with foundations, soil, rock, earth, or

any other geotechnical material, as an integral part of man-made product, structure, or system.

  - Normal Direction:  Direction perpendicular to the plane of a geotextile.

  - Permittivity:  Volumetric flow rate of water per unit cross sectional area per unit head under laminar flow conditions, in the normal direction through a geotextile.

  - Permeability:  Rate of flow of a liquid under a differential pressure through a material.

  - Transmissivity:  Flow or amount of liquid water per foot of material width passing through composite system at certain maximum soil pressure against geotextile at defined hydraulic gradient.

1.04 SUBMITTALS

- Product Data:  Manufacturer’s product data and installation instructions.

1.      Contact Manufacturer for installation instructions specific for field base.

02620-1

- Samples:  Submit minimum 12” x 12” product sample.

- Test Reports:  Submit test reports from an independent testing laboratory to verify

that product meets or exceeds specified physical properties.

  - QUALITY ASSURANCE

- Prior to installation of J-DRain Turfcore, review all installation instructions and details with an authorized representative of JDR ENTERPRISES, INC.

- Installation to be performed by certified installer or factory representative present.

  - DELIVERY, STORAGE, AND HANDLING

- Packaging and shipping:  Provide materials in original unopened containers with

manufacturer’s labels intact and legible.

- Acceptance at site:

  - Unload materials and check for damage.

  - Damaged materials determined by visual inspection will not be accepted.

  - Remove rejected materials from site immediately.

- Storage and protection.

  - Store materials in dry area in manufacturer’s protective packaging.

  - Store materials under cover, off ground and protect from extended sunlight.

- PART 2 – PRODUCTS

  - MANUFACTURED UNITS

- Acceptable manufacturers:

  - Products specified as standard of quality (J-DRain Turfcore) manufactured by:

JDR ENTERPRISES, INC., 292 South Main Street, Suite 200,

Alpharetta, Georgia 30009.  Telephone:  800-843-7569 or

770-442-1461. Fax:  770-664-7951.  Website: www.j-drain.com

2.    J-DRain Accessories:

a.    Splice Sheet:  For splicing J-DRain Turfcore end to end.

b.    Splice Fabric:  For covering butt joint splices and overlap splices

c.     Double sided tape:  For securing overlapping  fabric to create a

monolithic surface with J-Drain Turfcore.

d.     Anchor Pins:  For holding J-DRain Turfcore in place for installation

of turf.

3.    Physical Properties – Drainage Core

a.    Polypropylene dimple core heat bonded to non-woven geotextile.

b.    Flow Rate:  23 gpm/ft width @ gradient = .1

c.    Compressive Strength:  21,000 psf

1. Support fully loaded Emergency Vehicle (16,000 lbs.) with           point load of 85 psi.

d.   Drainage blanket will have core incorporating flex control joints

02620-2

4.    Physical Properties – Geotextile

a.    Puncture: 65 lbs.

b.    Mullen Burst:  210 psi

c.    AOS:  70 U.S. Sieve

d.    Permeability of geotextile:  140 gpm/sf

e.    Ultraviolet resistance:  70% at 500 hours

5.   Roll properties:

a.    Roll Length:  made to order up to 275 ft.

b.    Roll Width:    4 ft. or 8 ft.

c.    Roll Weight:   .2 lbs/sqare ft. – TBD by roll size

- PART 3 – EXECUTION

  - EXAMINATION

- Verifications of site conditions:

  - Verify that site is properly prepared for installation of J-DRain Turfcore.

  - Complete all excavation, fill, filter fabric placement, sideline trenches and headers, placement of course and fine aggregates, and leveling and compaction.

  - INSTALLATION

- All installation details and instructions are in strict accordance with the details and instructions of JDR ENTERPRISES, INC.

  - TURF INSTALLATION

- Turf installation should be in strict accordance with details and instructions of Turf Manufacturer.

- Minimum of 4-6 lbs. per square foot of infill required.

02620-3